WEAVING YARN CALCULATION

Complete Formula & Calculation Reference Guide

# 1. Default Input Parameters

These are fixed baseline values used throughout all calculations. They can be adjusted based on count and quality requirements.

| Parameter | Default Value | Purpose |
| --- | --- | --- |
| Grey Reed Add | 4 | Extra reed allowance added for grey (unfinished) fabric |
| Reed Less | 8 | Reed reduction based on yarn count & quality |
| Fabric Width Reed Add | 4 | Additional reed allowance for fabric width calculation |
| Pick Less | 4 | Reduction in picks for on-loom setting |
| Warp Yarn Calc Parameter | 1690 | Standard conversion constant for warp yarn KGS calculation |
| Dyeing Loss % | 5% | Default yarn loss during dyeing process |

# 2. Order & Meterage Calculation

This section calculates the total metres of warp and weft yarn required based on the buyer's order quantity.

| Field | Formula | Example Value |
| --- | --- | --- |
| Order Mtr | Buyer input | 60 mtr |
| Excess Mtr | Buffer quantity (optional) | - |
| Total Order Mtr | Order Mtr + Excess Mtr | 60 mtr |
| Warp Mtr (Bottom) | Total Order Mtr x (1 + Crimp% + Shrinkage%) | 120 mtr |
| Prod Mtr (Weft) | Production metres for weft calculation | 90 mtr |
| Top Warp Mtr | Same logic as Bottom Warp Mtr | 120 mtr |

# 3. Crimp % and Shrinkage %

These percentages measure how much the fabric contracts during weaving and processing. They are critical for accurate yarn ordering.

## 3.1 Bottom Warp Crimp %

Measures how much the warp yarn 'crimps' as it interlaces with the weft thread during weaving.

Bottom Warp Crimp % = (Warp Mtr - Fabric Mtr) / Fabric Mtr x 100

## 3.2 Shrinkage %

Measures how much the fabric shrinks after wet processing (washing, finishing, etc.).

Shrinkage % = (Fabric Mtr - Total Order Mtr) / Total Order Mtr x 100

## 3.3 Top Warp Crimp %

Same as bottom warp crimp, but calculated for the top beam in double-beam looms.

Top Warp Crimp % = (Top Warp Mtr - Fabric Mtr) / Fabric Mtr x 100

# 4. Reed Calculations

The reed is the comb-like device on the loom that spaces and separates the warp threads. Reed calculations determine the correct loom settings.

| Field | Formula | Example Value |
| --- | --- | --- |
| Finished Reed | Input (based on fabric spec) | 80 |
| Grey Reed | Onloom Reed + Grey Reed Add (4) | 76 |
| Onloom Reed | Finished Reed - Reed Less (8) | 72 |
| Finished Pick | Input (based on fabric spec) | 72 |
| Onloom Pick | Finished Pick - Pick Less (4) | 68 |
| Total Ends (Manual) | Finished Reed x Finished Width (inch) | 4,104 |
| Total Ends (Auto) | Calculated automatically by formula | 4,560 |
| Reed Space | Total Ends / Onloom Reed | 63.33 inches |
| Fabric Width (Grey) | Total Ends / (Onloom Reed + Grey Reed Add) | 60 inches |

# 5. Design Ends Finding

Used to determine how many warp ends fit within a specific measurement in millimetres. Useful for design repeat planning.

Key conversions:

- 1 Inch = 25.4 MM

- 1 MTR = 39.37 Inches

Required Ends = (Required MM / 25.4) x Finished Reed

Example: Required MM = 3 → Required Ends = (3 / 25.4) x 80 = 10 ends

# 6. Reed / Dent Calculation Table

This table shows how many ends (threads) pass through each dent of the reed, and the resulting EPI (Ends Per Inch).

| Reed Type | Dents per Inch | Ends per Dent | Total EPI |
| --- | --- | --- | --- |
| R3 | 1.5 | 64 | 96 |
| R4 | 2.0 | 72 | 144 |

EPI (Ends Per Inch) = Reed dents x Ends per dent — controls warp thread density in the fabric.

# 7. Warp Yarn Calculation (KGS)

This section calculates how many kilograms of warp yarn are needed for each colour, including a buffer for dyeing losses.

## 7.1 Required KGS Formula

REQ KGS = Ends x 1.094 / 1848 / Warp Count x Warp Mtr

Where:

- 1.094 = Conversion factor (yards to metres)

- 1848 = Hanks per kg constant for yarn count system

- Warp Count = Yarn count (e.g. 20s, 40s)

- Warp Mtr = Total warp metres required

## 7.2 With Dyeing Loss

With Dyeing Loss KGS = REQ KGS / (1 - Dyeing Loss %)

Extra yarn is ordered to compensate for losses during the dyeing process (default 5%).

## 7.3 Example (CREAM colour)

| Colour | Count | Ends | REQ KGS | With Dyeing Loss | Rounded |
| --- | --- | --- | --- | --- | --- |
| CREAM | 20s | 1,235 | 4.38 | 4.60 | 5 KGS |
| L.GREY | 20s | 298 | 1.06 | 1.11 | 1 KGS |
| D.GREY | 20s | 885 | 3.14 | 3.30 | 3 KGS |
| BLACK | 20s | 546 | 1.94 | 2.04 | 2 KGS |

# 8. Weft Yarn Calculation (KGS)

Calculates the weft (filling thread) yarn needed per colour for the full order quantity.

## 8.1 Weft Ends Calculation

Weft Ends = Onloom Pick x (Reed Space + 3 inches selvage)

3 inches is added as selvage allowance on both sides of the fabric.

## 8.2 KGS per Colour

Total per colour = (Colour Ends / Total Weft Ends) x Total Weft Length

Dyeing loss is then added in the same way as warp yarn:

With Dyeing Loss KGS = REQ KGS / (1 - Dyeing Loss %)

## 8.3 Example

| Colour | Count | Weft Ends | REQ KGS | With Dyeing Loss | Rounded |
| --- | --- | --- | --- | --- | --- |
| CREAM | 20s | 70 | 4.69 | 4.93 | 5 KGS |
| L.GREY | 20s | 14 | 0.94 | 0.99 | 1 KGS |
| D.GREY | 20s | 48 | 3.22 | 3.38 | 3 KGS |
| BLACK | 20s | 30 | 2.01 | 2.11 | 2 KGS |

# 9. Dyeing Loss & Issued KGS Tracking

This section tracks the actual yarn issued to the dyehouse versus what was received back, to monitor real dyeing losses.

| Field | Formula | Example Value |
| --- | --- | --- |
| Total Issued KGS | Total yarn sent to dyehouse | 192.56 KGS |
| Received KGS | Yarn received after dyeing | 186.70 KGS |
| Balance KGS | Issued - Received | 5.86 KGS |
| Dyeing Loss % | (Issued - Received) / Issued x 100 | ~3.04% |

# 10. Weaving Crimp & Processing Shrinkage

These calculations track fabric dimensional changes through the entire production process.

## 10.1 Weaving Crimp %

Measures fabric length loss during the actual weaving process.

Weaving Crimp % = (Warp Mtr - Weav Mtr) / Warp Mtr x 100

## 10.2 Processing Shrinkage %

Measures fabric length loss during wet processing (washing, finishing).

Processing Shrinkage % = (Grey Mtr - Processed Mtr) / Grey Mtr x 100

## 10.3 Example Values

| Stage | Metres | Loss |
| --- | --- | --- |
| Grey (after weaving) | 3,689.7 mtr | - |
| Processed (after finishing) | 3,364.2 mtr | 325.5 mtr |
| Processing Shrinkage % | - | 8.82% |

# 11. GSM and GLM Calculation

GSM (Grams per Square Metre) and GLM (Grams per Linear Metre) measure the weight of the fabric.

## 11.1 GSM Formula

GSM = ((EPI / Warp Count) + (PPI / Weft Count)) x 25.4

Where:

- EPI = Ends Per Inch (warp thread density)

- PPI = Picks Per Inch (weft thread density)

- 25.4 = Conversion factor for metric system

## 11.2 GLM Formula

GLM = GSM x (Fabric Width / 39.37)

GLM gives the weight of one metre length of fabric at the full fabric width.

# 12. GST Calculation (Sheet 2)

Calculates Indian Goods & Services Tax for textile invoicing.

| GST Type | Applicability | Rate | Components |
| --- | --- | --- | --- |
| Intra-State GST | Within same state | 5% total | SGST 2.5% + CGST 2.5% |
| Inter-State GST | Between states | 18% | IGST 18% |

SGST = Taxable Value x 2.5%

CGST = Taxable Value x 2.5%

IGST = Taxable Value x 18%

Grand Total = Taxable Value + Tax Amount

# 13. Resultant Count Calculation

When yarn is plied (twisted together), the resultant count determines the effective yarn thickness.

Resultant Count = Single Yarn Count / Number of Plies

| Yarn | Single Count | Plies | Resultant Count |
| --- | --- | --- | --- |
| 2/60s | 60s | 2 | 30s |
| 2/40s | 40s | 2 | 20s |

# 14. Bale Packing Tolerance

A standard tolerance is applied to dispatch quantities to account for small variations in fabric length during rolling and packing.

| Parameter | Value |
| --- | --- |
| Default Tolerance | +/- 8% |
| Tolerance Calculation | Order Mtr x Tolerance % |
| Max Dispatch Mtr | Order Mtr + (Order Mtr x 8%) |
| Min Dispatch Mtr | Order Mtr - (Order Mtr x 8%) |

# 15. Key Terms Reference

| Term | Full Form | Meaning |
| --- | --- | --- |
| EPI | Ends Per Inch | Number of warp threads per inch - controls warp density |
| PPI | Picks Per Inch | Number of weft threads per inch - controls weft density |
| GSM | Grams Per Square Metre | Fabric weight measurement |
| GLM | Grams Per Linear Metre | Weight of one metre length of fabric |
| Reed | N/A | Comb-like device on loom that spaces warp threads |
| Crimp | N/A | Waviness of yarn as it interlaces - causes length loss |
| Selvage | N/A | The woven edges on both sides of the fabric (3 inches added) |
| Beam | N/A | Roll on which warp yarn is wound before weaving |
| Grey Fabric | N/A | Fabric as it comes off the loom, before processing |
| Dyeing Loss | N/A | Yarn weight lost during the dyeing process |
| SGST/CGST | State/Central GST | Intra-state tax split equally between state and center |
| IGST | Integrated GST | Single tax for inter-state transactions |

Weaving Yarn Calculation Reference | All formulas based on ORIGINAL sheet data